## Slide 1: Cyclotron Resonance and Faraday Rotation in infrared spectroscopy
PHYS 211A
Yinming Shao

## Slide 2: Outline
Cyclotron resonance
  Application in Ge: determing effective mass
  Experimental detection of cyclotron resonance using FTIR
Faraday Rotation
  General expression
  Experimental detection
Giant Faraday Rotation in Graphene

## Slide 3: Cyclotron resonance
Apply oscillating in-plane E-field
Charges can resonantly absorb energy from E-field
Resonance condition
Typically changing B field around resonance
B
- e
+ e
G. Dresselhaus et al., Phys. Rev. 98, 368 (1955)
q
Using microwaves as
AC E-field
Notes: Charge carriers will do cyclotron motion when magnetic field is present

## Slide 4: A word on different masses
Resonance condition
is the cyclotron mass :
Effective mass:
S is the
k-space area of cyclotron orbits
Parabolic bands:
Graphene:
vanishes
exists!

## Slide 5: Cyclotron Resonance (CR) in Ge
G. Dresselhaus et al., Phys. Rev. 98, 368 (1955)
In general, effective mass are anisotropic,
For Ge, constant energy surfaces near band edge are spheroidal
Measuring CR at different field angles
2. Extract cyclotron mass by

## Slide 6: Condition to observe cyclotron resonance
Carrier mobility:
For 1 T field,
Requires
Need high purity samples to see CR!!
Ge is the first high purity sample
people could obtain in ~1945
Organic semiconductors for CR??
Long way…
Metals have high conductivities and
E-field cannot penetrate sample requires special geometry
Resonance condition is easier to realize in
THz ( Hz) and far-infrared frequencies.
(FFT algorithm become popular after ~1965)
Commercial superconducting magnet  ~10 T B-field in lab accessible (~late 60s)
Use FTIR based
transmission to see CR

## Slide 7: Fourier Transform InfraRed Spectroscopy (FTIR)
Based on a two-beam Michelson Interferometer:
Infrared source broad band light source
Beam-splitter divides the beam to two with similar intensity
Fixed mirror, moving mirror  change the optical path difference
               interferogram
Transmission
set-up
Fourier transform the to get the spectrum

## Slide 8: Fourier Transform InfraRed Spectroscopy (FTIR)
Advantage:
1. Fast: obtain transmittance/reflectance spectrum over a broad frequency range rapidly
Simple: moving mirror is the only moving part in the system
Sensitive: bright light source; average multiple scans is fast
http://mmrc.caltech.edu/FTIR/FTIRintro.pdf

## Slide 9: CR in graphene from transmittance measurements
Transmission data normalized by 0T data
 Cancel out features that are not field dependent
Power absorption:
It can be shown that the Half Width at Half
Maximum is about the scattering rate .
Recall that , by fitting the
cyclotron frequency one get estimates about
Carrier mobility.
I. Crassee et al, Nat Phys 7, 48 (2011)
Estimate mobility
Contact free!

## Slide 10: Magneto-Optical Faraday Effect
First observation (in 1845) of
light-magnetism interaction!
Optically active material:
Field induced circular birefringence
For linearly polarized light, the polarization
plane of the transmitted light is rotated
Notes: Some nature material

## Slide 11: Faraday rotation
http://cddemo.szialab.org/
left- and right-handed light
travel at different
speeds in the medium
Complex refractive index
Circular Birefringence

## Slide 12: General expression of Faraday rotation angle: Single passage approximation
Need Relatively thick sample
to suppress multiple reflection
Complex transmission:
Faraday rotation:

## Slide 13: Detecting Giant Faraday rotation using crossed polarizers
The most straightforward method
Polarizer
Analyzer
Rotate the analyzer from 0 to 180 and then
Fit the transmitted intensity with
Combine with FTIR
Faraday rotation
at different frequencies

## Slide 14: Giant Faraday rotation in graphene (on SiC)
Negative slope  hole doping!
I. Crassee et al, Nat Phys 7, 48 (2011)
is maximized around
Sign of
Matches the sign of
1 atomic layer ()
 > 6 degrees of polarization change!
Definitely Giant
Typical semiconductors (e.g. InSb)
comparable rotation but several
magnitudes thicker ()

## Slide 15: Some modeling based on Drude model
Assuming an harmonically varying field:
and therefore drift velocity
Equation of motion:
EOM becomes:
Solve v in terms of E and B then compared to
Current density
Dynamical conductivity (magnetic field introduces anisotropy)

## Slide 16: Explicit form of dynamical conductivity
even function of
odd function of

## Slide 17: Modeling off-diagonal conductivity
Real part
Real part of () changes sign
around cyclotron frequency.
Its derivative around matches the
sign of
gives information about the carrier type!
 Similar to DC Hall effect
1. Real part of () is maximized
around cyclotron frequency.
Its derivative is maximized at
Modeling graphene as a two dimensional
electron gas, its Faraday rotation angle
Is proportional to Re() up to some positive
constant

## Slide 18: Giant Faraday rotation in graphene
Negative slope  CR involves hole states
(Fermi level in valence band)
I. Crassee et al, Nat Phys 7, 48 (2011)
Faraday rotation is enhanced
near cyclotron resonance  Giant

## Slide 19: Landau Level transitions in MLG (on SiC)
Positive slope indicates
The observed LL transition
Involves electron like states.
Unlike single layer graphene,
multilayer graphene are less doped and fall in
the quantum regime CR LL transitions

## Slide 20: Summary
Cyclotron resonance is powerful for determining effective mass in semiconductors and estimate carrier mobility
Faraday Rotation is the optical analogue of Hall effect and is enhanced around cyclotron resonance
FTIR based CR and FR extends traditional measurements to much broader frequency range
Thanks for your attention!